● Product center－catalog, introduction

● QB-AL series Aluminum base copper clad laminate

Features：

●  Excellent thermal conductivity

- Excellent insulating ability

- Excellent dimensional stability

- Excellent Machinability

- Excellent electromagnetic shielding

- High quality but low price

Applications：

- LED lighting

- Thick film hybrid integrated circuits

- Power supply

- Solid Relay

Performance：

| Item | Test condition | Units | Index |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | T-100 | T-100-G | T-101 |
| Thermal Conductibility | A | W/m·k | 1.3～1.8 | 1.1～1.8 | 1.5～2.0 |
| Peel Strength | A After thermal stress | N/mm | 1.8 1.8 | 1.5 1.5 | 1.5 1.5 |
| Thermal stress | 288℃ | S | 60S No-delimitation, No-blistering | 30S No-delimitation, No-blistering | 90S No-delimitation, No-blistering |
| Surface Resistance | C-96/35/90 E-24/125 | MΩ | 107 106 | 106 105 | 107 107 |
| Volume Resistivity | C-96/35/90 E-24/125 | MΩ·cm | 108 106 | 107 105 | 108 107 |
| Electrical strengthen | A | KV/mm | 40 | 30 | 30 |
| Flammability | UL94 | — | V-0 | V-0 | V-0 |
| Warping | A | % | 0.2 | 0.5 | 0.15 |
| Moisture absorption | D-24/23 | % | 0.05 | 0.1 | 0.05 |
| CTI | IEC60112 | V | 175 | 175 | 200 |

| Item | Test condition | Units | Index |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | T-111 | T-112 | T-113 | T-114 |
| Thermal Conductibility | A | W/m·k | 1.8～3.0 | 2.5～5.0 | 1.5～2.0 | 1.5～2.0 |
| Peel Strength | A After thermal stress | N/mm | 1.5 1.5 | 1.3 1.3 | 1.3 1.3 | 1.3 1.3 |
| Thermal stress | 288℃ | S | 60S No-delimitation, No-blistering | 60S No-delimitation, No-blistering | 600S No-delimitation, No-blistering | 600S No-delimitation, No-blistering |
| Surface Resistance | C-96/35/90 E-24/125 | MΩ | 107 106 | 107 106 | 108 108 | 108 108 |
| Volume Resistivity | C-96/35/90 E-24/125 | MΩ·cm | 108 106 | 108 106 | 108 108 | 108 108 |
| Electrical strengthen | A | KV/mm | 30 | 30 | 30 | 30 |
| Flammability | UL94 | — | V-0 | V-0 | V-0 | V-0 |
| Warping | A | % | 0.15 | 0.15 | 0.15 | 0.15 |
| Water Absorption | D-24/23 | % | 0.05 | 0.05 | 0.05 | 0.05 |
| CTI | IEC60112 | V | 175 | 175 | — | — |